## Slide 1: Fracture of Lattice Metamaterials
By: Helder Rebelo

## Slide 2: 3D Toughness of Mechanical Metamaterials (Nature Materials, 2022) ~ Summary
K alone is insufficient in architected lattices; a two‑parameter description using (K, T) with crack‑size/load‑path calibration captures failure across stretching vs buckling regimes.

## Slide 3: Bridge to 2D: What carries over? What changes?
K‑dominant fields persist in planar beam‑lattices, but topology (connectivity) dictates local fields and failure sites.
T‑stress sensitivity remains important for apparent Kc and mechanism switching (tension fracture ↔ elastic buckling).
Scaling with relative density (ρ̄): triangular ≈ ρ̄; hexagonal (bending) ≈ ρ̄²; kagome often ≈ ρ̄1/2 to ρ̄, depending on failure criterion.
Specimens: center‑cracked plates & boundary‑layer domains avoid boundary artifacts; embedded flaws over through‑thickness when possible.
Fleck & Qiu (2007); Romijn & Fleck (2007); Tankasala et al. (2015); Omidi & St‑Pierre (2023).

## Slide 4: 2D Fracture Modelling & Approaches That Work
Boundary‑Layer (BL) Method
Impose analytical u(r,θ) for target KI/KII (and optional T) on a circular ring of perimeter nodes.
Increase K until first local criterion met → Kc; sweep mixity to generate a mixed‑mode envelope.
Fleck & Qiu, 2007; Tankasala et al., 2015.
Beam‑Lattice FE + Progressive Failure
Model struts with Euler/Timoshenko beams; brittle (εf) or plastic (J2) cell‑wall law.
Embedded pre‑crack; BL or far‑field traction BCs; element removal/softening for crack growth & R curves.
Hsieh et al., 2020; Omidi & St‑Pierre, 2023.
Analytical / Reduced Models
Square/triangular/kagome beam networks: closed form relations for Kc(ρ̄) and imperfection sensitivity.
Fuse‑network analogs for antiplane fracture & size effects.
Romijn & Fleck, 2007; Nguyen 2024 (fuse nets).

## Slide 5: What 2D Studies Consistently Find
Topology matters: Kagome & demi‑regular can outperform triangular under Mode II; triangular excels in Mode I for stretching dominated structures.
Scaling: K̄c ≡ Kc/(σf√ℓ) often follows A·ρ̄ⁿ with n≈1 (triangular), n≈2 (hex), n ≈ ½–1 (kagome/demi‑regular).
Initiation site: can be off the crack plane (kagome) due to elastic blunting regions extending O(10ℓ).
Mixed‑mode envelopes: BL studies show topology‑dependent envelopes (near‑circular vs piecewise) and strong T‑stress effects.
Fleck & Qiu, 2007; Romijn & Fleck, 2007; Tankasala et al., 2015; Omidi & St‑Pierre, 2023.

## Slide 6: Setup & Boundary Conditions (Omidi & St-Pierre, 2023)
Goal: predict where the crack will propagate next by finding the first failing strut under a clean near-tip field.
Model: 2D beam-lattice of demi-regular topologies; unit-cell size ℓ vary relative density ρ​ by changing strut thickness t at fixed ℓ. Crack is a notch along x with the tip at the origin; crack faces are traction-free.
Domain & BCs: use a boundary-layer (BL) domain (big enough that the outer boundary doesn’t contaminate the tip). Prescribe the LEFM Mode I/II displacement field on the outer ring nodes: choose a mixite ψ=tan^−1(KII/KI) and ramp the amplitude K. This reproduces the near-tip solution inside the lattice.
Elements & material: Euler/Timoshenko beam elements; elastic-brittle struts with tensile strength (or failure strain). Local mesh refinement near the crack tip.

## Slide 7: Setup & Boundary Conditions (Omidi & St-Pierre, 2023) Cont.
Load ramp & criterion: increase K at fixed ψ. After each increment, compute strut resultants; when any strut first reaches the strength criterion, record that increment as Kc​ and record that element’s location this is the predicted next tip (initiation site).
Mixed-mode envelope: repeat across ψ∈[0∘,90∘] to build Kc(ψ). Annotate each envelope segment by the initiation site (on-plane vs off-plane). These labels map where the crack is expected to propagate from under each mixite.
Scope & extensions: this procedure targets initiation (first failure). For R-curves / growth, extend with progressive element removal/softening under the same BL setup.

## Slide 8: References
Shaikeea AJD et al., Nature Materials (2022): article
Fleck NA & Qiu X., JMPS (2007): pdf
Romijn NER & Fleck NA, JMPS (2007): pdf
Tankasala HC, Deshpande VS, Fleck NA, J. Appl. Mech. (2015): pdf
Omidi M & St‑Pierre L, Scripta Materialia (2023, CC BY): open page
Montemayor LC et al., Sci. Reports (2016): article
Gao Z et al., Nat. Communications (2024): article