## Slide 1
NSF REU — OPTICS & PHOTONICS | SUMMER 2026
Predicting Lattice Stiffness with
Graph Neural Networks
A fast, defect-aware alternative to finite element simulation for architected lattice materials
Alexander Adams
Dept. of Mechanical Engineering & Materials Science, University of Pittsburgh
Advisor: Dr. Xing Liu
Dept. of Mechanical & Industrial Engineering, New Jersey Institute of Technology
Notes: Title slide. Introduce project, myself, and my advisor. Keep it to about 15 seconds.

## Slide 2
Problem, Significance & Goals
The Problem
Theory assumes perfectly periodic lattices. Manufacturing reality introduces strut-diameter variation, missing struts, and node misalignment — so classical models fail to predict real stiffness and fracture behavior.
Project Goal
Build a graph neural network that predicts lattice stiffness directly from imperfect, real-world geometry — fast enough for iterative design, accurate enough to trust in place of full simulation.
ADVANCED MATERIALS: THE MONEY BEHIND THE MATH
$1.2T+
Global advanced materials market (2023)
$110–133B → $205–313B
Architected composites & lattice materials, 2024 → 2032–34 (~8–9% CAGR)
30–50% / 40%+
Stiffness-to-weight gain over foams / possible weight reduction from lattice design
Notes: Frame the problem, then pivot to the size of the prize: cite the $1.2T+ advanced materials market and the faster-growing lattice/composites segment. Land the line: materials set the ceiling for every field.

## Slide 3
The Materials Ceiling
Every high-stakes field runs into the same wall — no matter how urgent the mission
Medicine
Neurodegenerative drug carriers and implants are only as good as the material that holds them together.
Energy
Battery density and solar efficiency stall without lighter, stronger structural and storage materials.
Aerospace
Every efficiency gain in flight is a materials problem before it is ever an aerodynamics problem.
Defense
Protection-to-weight ratio is dictated by the material itself, not by the mission built around it.
Alzheimer’s therapeutics. Clean energy. Hypersonic flight. Every one of them stalls at the same wall — what materials can actually do. This project is built to move that wall.
$1.2T+ global advanced materials market underwrites all four — this is not a niche problem.
Notes: This is the pitch slide: don't apologize for not curing a disease directly — make the case that every headline field, including medicine, is capped by materials, and that's exactly the bottleneck this project attacks. Land the pull-quote slowly, then move on.

## Slide 4
Research Approach
A graph neural network learns directly on lattice geometry — no meshing, no billions of degrees of freedom
Lattice Geometry
Node positions,
connectivity, boundary
conditions
▸
Graph Construction
Weighted edges,
rich node + graph-level
features
▸
GCN Model
Message passing over
graph structure learns
stiffness response
▸
Predicted Stiffness
Fast surrogate for
full FE simulation
Iterative Pipeline Development
Weighted graph edges
Richer node features
Graph-level features
Target normalization
Architecture search (GCN-2/3, GraphSAGE, GIN)
Multi-seed validation
Each step keeps Adam optimization + the same train/validation/test split fixed, so gains are attributable to representation, not tuning noise.
Notes: Walk through the pipeline left to right, then point out the six representation upgrades tested this summer. Emphasize this is a controlled, additive research process.

## Slide 5
Best Model: GCN-3 Architecture
Richer node features → edge-weighted GCN convolutions → graph-level fusion → normalized stiffness output · mean test R² 0.9456
INPUT — Node Features (×9)
x, y, degree, weighted degree, dist. to center, boundary flag, mean/max edge length, mean edge weight
INPUT — Weighted Edges
Adjacency-area edge weights replace binary connectivity; passed into every GCNConv layer
▾
3 × GCNConv — hidden_dim = 24 — ReLU + Dropout (0.10) — edge-weighted message passing
Layer 1
9 → 24
▸
Layer 2
24 → 24
▸
Layer 3
24 → 24
▾
Global Mean Pooling
Node embeddings → one 24-dim graph embedding per lattice
+ Graph-Level Features (×12)
node/edge counts, density, edge-weight & degree stats, center-distance stats — concatenated after pooling
▾
concat → 36-dim
Linear Output Layer → normalized stiffness prediction → inverse-transform → Predicted Stiffness
TRAINING CONFIGURATION
Optimizer: Adam, two-phase LR
0.003 → 0.0005
Weight decay:
1e-5
Dropout:
0.10
Hidden dim:
24
Schedule:
200 + 700 epochs
WHY THIS CONFIG WON
3 layers beat 2 in 4 of 5 seeds — modest but real depth gain
GraphSAGE and GIN did not outperform GCN
Mean test R²: 0.9456 · RMSE: 0.002882
Prediction-set generalization is the open frontier — residual variants trade test accuracy for it
Notes: Walk down the diagram top to bottom: 9 node features and weighted edges go into 3 stacked GCNConv layers (hidden dim 24), pool to a graph embedding, fuse with 12 graph-level features, then a linear layer predicts normalized stiffness. Mention Adam two-phase schedule and why GCN-3 was promoted over GCN-2/GraphSAGE/GIN.

## Slide 6
Results
Representation upgrades — not optimizer tuning — drove the accuracy gain
Chart: Mean Held-Out Test R² by Configuration
| Baseline GCN-2 | + Richer Features | + Graph Features | + Target Norm. | GCN-3 (best)
Test R² | 0.9148 | 0.938 | 0.9411 | 0.9447 | 0.9456
R²: 0.9148 → 0.9456
Baseline vs. best multi-seed configuration
RMSE: 0.00382 → 0.00288 (−24%)
Validated Across 5 Seeds
Test R² range: 0.934 – 0.955
Adam remains the strongest optimizer — AdamW and SGD variants underperform
GCN-3 modestly outperforms GCN-2; GraphSAGE and GIN did not improve results
Open question: out-of-distribution (prediction-set) generalization still trails held-out test accuracy — the focus of ongoing work.
Notes: Point at the chart: each bar is a confirmed, multi-seed-validated gain. Baseline R2 0.9148 to 0.9456 with 24% RMSE reduction. All gains from feature engineering, not optimizer swaps.

## Slide 7
Discussion & Future Work
Where this stands
A fast, defect-aware GCN surrogate now predicts lattice stiffness at 0.95 test R² — replacing costly FE simulation and enabling rapid design iteration across defective, real-world lattice geometries.
Next steps
Multi-seed validation of Huber-loss objective for tail-seed stability
Stabilize residual GCN-3 to close the out-of-distribution gap
Extend beyond stiffness to failure-mode / fracture prediction
THE BIGGER PICTURE
Materials set the ceiling for aerospace, energy, medicine, and defense alike. Faster, defect-aware design tools push that ceiling higher — across a $1.2T+ market moving toward $200–300B+ in architected materials alone.
ACKNOWLEDGEMENT
Dr. Xing Liu
Dept. of Mechanical & Industrial Engineering, NJIT
NSF REU Site: Optics & Photonics
New Jersey Institute of Technology, Summer 2026
Notes: Close by restating the significance in one sentence, thank Dr. Liu and the REU program, and stop — leave time for questions.